## Slide 1: Under Graduate Project (UGP) Catalyst Synthesis For Hydrodesulfurization Using Varied Silica Supports
By : Bhavishya Gupta (220295) Under the Guidance of Prof. Sri Sivakumar
Mentored by Dhyananand Sir
Indian Institute Of Technology (IIT) Kanpur

## Slide 2: Hydrodesulfurization (HDS)
What is Hydrodesulfurization?
A catalytic process that removes sulfur from petroleum products by reacting sulfur compounds with hydrogen, forming hydrogen sulfide (H2S).In HDS OF DBT, Dibenzothiophene reacts with hydrogen to form Biphenyl and hydrogen sulphide.
Key Reaction
C12H8S + 2H2 → C12H10 + H2S
(1)
Why is HDS Important?
Reduces sulfur emissions. - Prevents catalyst poisoning in refining.
Ensures fuel quality compliance.

## Slide 3: Challenges in DBT Hydrodesulfurization
Major Challenges
Steric Hindrance: The rigid, fused-ring structure of dibenzothiophene (DBT) reduces catalyst accessibility, making sulfur removal more challenging.
Low Reactivity: DBT has strong C–S bonds that require high temperatures (300–400°C) and severe hydrogenation conditions for effective desulfurization.
Catalyst Deactivation: Sulfur compounds and coke formation progressively poison the catalyst, reducing its lifespan and efficiency.
Hydrogen Demand: A significant amount of hydrogen is required to break sulfur bonds, increasing both operational costs and process complexity.

## Slide 4: Pelletization and Sieving in Catalyst Synthesis
Pelletization
The process of forming uniform catalyst pellets by mixing components with a binder, pressing them into shape, drying, and calcining to harden them. Ensures consistent size and shape for even distribution and efficiency in the reactor.
Sieving
Separates particles based on size using a mesh to achieve uniform particle distribution. This prevents clogging and ensures consistent catalytic activity for optimal reactor performance.

## Slide 5: Reactor Filling Process
Objective
Load the reactor with catalyst and support material for uniform flow, minimal channeling, and reactor protection.
Catalyst Preparation: Pelletized and sieved for uniform size.
Coswool as Barrier: Used for cushioning but causes itching if handled barehanded.
Layering: Coswool → Gamma Al2O3 (support) → Catalyst →
Coswool → Gamma Al2O3.
Filling Method: Small portions, vibration techniques to remove voids.
Final Steps: Tighten bolts, conduct helium leakage test, and verify with a soap bubble test.

## Slide 6: Amorphous Alumina Preparation
Step 1: Solution Preparation
Measured 3.679 g of Al(NO3)3, 9H2O and added it to a 3-neck flask containing 15 ml of oleylamine (OAM) solution, which acts as a solvent.
Step 2: Addition of Reducing Agents
Added 0.5 ml each of Oleic Acid and Tri-octyl phosphate (TOP) to the prepared solution, which serve as reducing agents.
Step 3: Thermal Decomposition
The solution was subjected to thermal decomposition by immersing the setup in an oil bath. The heating rate was 1.5◦C - 2◦C per minute, starting from 30◦C to 250◦C, and then cooled to room temperature.

## Slide 7: Washing Procedure for Pure Amorphous Alumina
Purification Steps
Step 1: Dissolution - Dissolved the overnight dried sample in 20-25 ml of toluene and transferred to Tarson A.
Step 2: Weight Balancing - Added distilled water to Tarson B to balance the weight of Tarson A (error < 0.005 g).
Step 3: Centrifugation - In centrifugation machine set the controls at 10000 rpm for 2 minutes, discarded the supernatant from Tarson A to the disposal bottle.
Step 4: Acetone Treatment - Added 40 ml of acetone to the precipitate and subjected to intense vibration using shakers and sonicator devices to form a homogeneous mixture.
Step 5: Repeating - Repeated the process from Step 2 three times to ensure purity.

## Slide 8: Support (Amorphous Alumina + Silica) Making Procedure
Step 1: Mixing
Measured amounts of amorphous alumina [am-Al2O3 (87%)] and silica [SiO2 (13%)] are mixed via attrition mixing using a mortar- pestle for about 20-30 minutes so that both gets mixed properly.
Step 2: Drying
Transferred the mixture to a small Tarson and covered it with alu- minum foil with small holes. Dried at 120◦ C in a heater overnight to remove moisture. Finally we will get the desired support material.

## Slide 9: Catalyst Making Procedure
Catalyst Preparation Steps
Step 1: Measuring Components - Measured the amount of cal- cined support formed and procured the relevant amounts of nickel nitrate [Ni (NO3)2.6H2O] and ammonium molybdate tetrahydrate [(NH4)6 Mo7O24.4H2O].
Step 2: Mixing Solution - The raw materials were mixed in a tarson in the presence of citric acid, forming a homogeneous solution.
Step 3: Impregnation - The mixed solution of salts was added dropwise onto the support (am-Al2O3 + 13% SiO2).
Step 4: Final Mixing and Calcination - Finally, the solution was kept for overnight mixing, ensuring wet impregnation of active ma- terials [Nickel(Ni) and Molybdenum(Mo) onto the support before calcination at 550◦ C with a 2◦ C/min ramp rate.

## Slide 10: Calculations and Results of Support and Catalysts
Overview
I have written MATLAB code to calculate the support and active material required to achieve a specific catalyst composition. The code includes comments for clarity, making it easy to modify for different catalyst weights.
Key Features
Well-commented for easy understanding Dynamic – can be modified for any catalyst weight Provides clear numerical results
Download the MATLAB Code
For detailed MATLAB calculations, click the link below:
Download MATLAB Code

## Slide 11: Status of the Work Done in Project
Project Status
Understood the importance of HDS Reactions and requirement of efficient catalysts
Understood the Catalyst filling procedure in the reactor.
Prepared 5 catalysts with varying active material concentrations:
▶ 15%, 20%, 30%, 35%, and 50%
Prepared 4 batches of Amorphous Alumina.
Remaining work: Synthesizing catalysts with three other varieties of silica.

## Slide 12: Reflections on the Project
Learning Experience
This project deepened my understanding of catalysis, especially the practical aspects of catalyst synthesis, bridging theory with hands-on experimentation.
Experimental Exposure
Conducting experiments firsthand exposed me to high-level re- search, helping me appreciate the precision and rigor behind scientific methodologies.
Gratitude
I sincerely thank Dhyananand Sir for his unwavering guidance and Professor Sri Sivakumar for this invaluable opportunity and mentor- ship.

## Slide 13: Thank You for Your Time and Attention!
Bhavishya Gupta (220295)
B.Tech, Chemical Engineering, IIT Kanpur 3rd Year Undergraduate
Email: bhavishyap22@iitk.ac.in